## Slide 1: HTGB & HTRB Life TEST FBG20N18

## Slide 2: DC LIFE
Tested variations of VDS and VGS voltages over several temperatures over a 2000Hrs timeframe
  VDS Tested : 200V, 230V, 250V at Temperatures of 100C and 130C
  VGS Tested : 6V, 6.75V, 7.25V at Temperatures of 100C and 150C
  Parts tested with full parametric test on Focused tester at interim steps 24hrs, 48,hrs, 96hrs, 210hrs, 500hrs, 1000hrs, 1500hrs, 2000hrs
  Parts with very high leakage were removed at each step
  X axis (voltage represents Applied stress voltage not test voltage)

## Slide 3: OVEN LOGS

## Slide 4: HTGB LIFE
IDSS tested at 200V

## Slide 5: HTGB LIFE
IGSSF tested at 5V

## Slide 6: HTGB
IGSSR tested at -4V

## Slide 7: HTGB
DRON pre at 15A VGS@5V

## Slide 8: HTGB
DRON post at 15A VGS@5V
10s stress at 160V followed by
Test at 5-8us after removal

## Slide 9: HTGB
RDSON at 18A VGS@5V

## Slide 10: HTGB
Vgsth at 3mA

## Slide 11: HTRB
IDSS tested at 200V

## Slide 12: HTRB
IGSS tested at 5V

## Slide 13: HTRB
IGSR tested at -4V

## Slide 14: HTRB
DRON pre at 15A VGS@5V

## Slide 15: HTRB
DRON post at 15A VGS@5V
10s stress at 160V followed by
Test at 5-8us after removal

## Slide 16: HTRB
RDSON at 18A VGS@5V

## Slide 17: HTRB
Vgsth at 3mA

## Slide 18: LIFE TEST SUMMARY HTGB
Temp | Stress V | Time(Hrs) | SN | Wafer # | Notes
100C | 6.75 |  |  |  | 
 |  | 1479 | 68 | Q211 | High IGSS, still functional-part was OOF
 |  | 2020 | 126 | Y003 | High IGSS, still functional-OOF replacemnt actual hours 1924
 | 7.25 | 96 | 81 | Q211 | Out of Family, High IGSS,IDSS, Vth - Part was OOF
 |  | 500 | 16 | Y046 | High IGSS -removed 1000Hrs
 |  | 1000 | 55 | Y003 | High IGSS, still functional
 |  |  | 60 | Q211 | High IGSS -removed 1000Hrs
 |  |  | 127 | Y003 | High IGSS, still functional
 |  | 1479 | 70 | Q211 | High IGSS, still functional-OOF replacment actual hours 1383
 |  | 2020 | 53 | Y003 | High IGSS, Vth, Idss nonfunctional
 |  |  | 59 | Q211 | High IGSS, Vth, Idss nonfunctional=Part was OOF
 |  |  | 61 | Q211 | High IGSS, low Vth, high Idss nonfunctional
 |  |  | 17 | Y046 | High IGSS, low Vth, high Idss nonfunctional
 |  | 2188 | 13 | Y046 | High IGSS, still functional
Temp | Stress V | Time(Hrs) | SN | Wafer # | Notes
150C | 6V |  |  |  | 
 | 6.75 | 1000 | 85 | Y003 | High IGSS, still functional
 |  | 2020 | 33 | Y046 | High IGSS, high Vth still functional
 |  | 2188 | 29 | Y046 | High Gate and Drain, Fuse Blew Pulled.
 | 7.25 | 48 | 39 | Q211 | High IGSS, still functional
 |  |  | 40 | Y046 | High IGSS, still functional
 |  | 138 | 37 | Y046 | High IGSS, IDSS, Low Vth
 |  | 210 | 42 | Q211 | High IGSS, still functional
 |  |  | 34 | Y046 | High IGSS, still functional-removed 100Hrs
 |  | 500 | 78 | Y003 | High IGSS, IDSS, High Vth
 |  | 1000 | 43 | Q211 | High IGSS, still functional
 |  |  | 44 | Q211 | High IGSS, still functional
 |  |  | 84 | Q211 | High IGSS, still functional
 |  |  | 35 | Y046 | High IGSS, still functional-removed 100Hrs
 |  |  | 40 | Y046 | High IGSS, still functional-removed 100Hrs
 |  |  | 75 | Y003 | High IGSS, still functional
 |  |  | 79 | Y003 | High IGSS, still functional-removed 100Hrs
 |  | 1479 | 130 | Y003 | High IGSS, still functional
 |  |  | 36 | Y046 | High IGSS, still functional
 |  | 2020 |  |  | No New Failures - 4 surviving parts 1 of which was OOF

## Slide 19: LIFE TEST SUMMARY HTRB
Temp | Stress V | Time(Hrs) | SN | Wafer # | Notes
100C | 200V |  |  |  | 
 | 230V | 1020 | 94 | Y003 | Fuse blown, pulled
 |  | 1526 | 90 | Y003 | Fuse blown, pulled
 |  |  | 110 | Q211 | Fuse blown, pulled
 | 250V | 24 | 119 | Q211 | Fuse blown, pulled
 |  | 48 | 121 | Y003 | Fuse blown, pulled
 |  | 500 | 117 | Q211 | Fuse blown, pulled
 |  | 1020 | 100 | Y003 | Fuse blown, pulled
 |  | 1526 | 101 | Y003 | Fuse blown, pulled
 |  | 2048 | 121 | Q211 | Fuse blown, pulled
 |  |  | 123 | Q211 | Fuse blown, pulled
Temp | Stress V | Time(Hrs) | SN | Wafer # | Notes
130C | 200V | 24 | 120 | Y003 | Fuse blown, pulled
 |  | 500 | 102 | Y003 | Fuse blown, pulled
 |  | 1020 | 105 | Y003 | Fuse blown, pulled
 |  | 1426 | 107 | Y003 | Fuse blown, pulled
 |  |  | 130 | Q211 | Fuse blown, pulled
 | 230V | 48 | 140 | Q211 | Fuse blown, pulled
 |  | 210 | 109 | Y003 | Fuse blown, pulled
 |  | 500 | 112 | Y003 | Fuse blown, pulled
 |  | 1020 | 119 | Y003 | Fuse blown, pulled
 |  | 1526 | 74 | Q211 | Fuse blown, pulled
 |  |  | 138 | Q211 | Fuse blown, pulled
* | No failures seen from wafer Y046 |  |  |  | 

## Slide 20: HTRB Failures XRAY 230V 100C
Y003 #94-PRE-POST
Q211 #110-PRE-POST
Y003 #90-PRE-POST

## Slide 21: HTRB Failures XRAY 250V 100C
Y003 #121-PRE POST
Q211 #119-PRE POST
Q211 #117-PRE POST

## Slide 22
HTRB Failures XRAY 250V 100C
Q211 #121-PRE POST
Y003 #100-PRE POST
Y003 #101-PRE POST

## Slide 23
HTRB Failures XRAY 250V 100C
Q211 #123-PRE POST

## Slide 24: HTRB Failures XRAY 200V 130C
Y003 #120-PRE POST
Y003 #102-PRE POST
Y003 #105-PRE POST

## Slide 25: HTRB Failures XRAY 200V 130C
Y003 #107-PRE POST
Q211 #130-PRE POST

## Slide 26: HTRB Failures XRAY 230V 130C
Q211 #140-PRE POST
Y003 #109-PRE POST
Y003 #112-PRE POST

## Slide 27: HTRB Failures XRAY 230V 130C
Y003 #119-PRE POST
Q211 #138-PRE POST
Q211 #74-PRE POST