## Slide 1: FBG20N18BSH Reliability Data
5/1/24

## Slide 2
FBG20N18BSH Switching Life Test
Tested variations of VDS voltage, IDS current and Switching Frequency in a high side buck converter over a 2000 hours time and across 3 wafer lots.
  VDS tested : 140V and 170V (Nominal) measured at Power supply and does not include any overshoot occurring at the DUT due to the buck circuit performance.
  Iout tested : 1A, 4A
  Parts tested with full parametric test at interim steps 48,hrs, 120hrs, 260hrs, 500hrs, 1000hrs, 2000hrs
  No failures have been observed thru 2000hrs

## Slide 3
FBG20N30BSH Circuit
The circuit was not optimized for efficiency but rather to demonstrate the stability of device and Rdson.
FBG20N18
Or
FBG10N30
Simplified High Side Buck converter circuit
FBG20N18
GAM01 Driver

## Slide 4
EFFICIENCY at 100kHz VDS=140V-170V Io=1A - 4A

## Slide 5
EFFICIENCY at 100kHz VDS=140V-170V Io=1A - 4A

## Slide 6
EFFICIENCY at 500kHz VDS=140V-170V Io=1A - 3A
Temp = ~60C

## Slide 7
EFFICIENCY at 500kHz VDS=140V-170V Io=1A - 3A

## Slide 8
FBG20N18 DC LIFE
Tested variations of VDS and VGS voltages over several temperatures over a 2000Hrs timeframe
  VDS Tested : 200V, 230V, 250V at Temperatures of 100C and 130C
  VGS Tested : 6V, 6.75V, 7.25V at Temperatures of 100C and 150C
  Parts tested with full parametric test on Focused tester at interim steps 24hrs, 48,hrs, 96hrs, 210hrs, 500hrs, 1000hrs, 1500hrs, 2000hrs
  Parts with very high leakage were removed at each step
  X axis (voltage represents Applied stress voltage not test voltage)

## Slide 9
FBG20N18 HTGB LIFE
9
IDSS tested at 200V

## Slide 10
FBG20N18 HTGB LIFE
10
IGSSF tested at 5V

## Slide 11
FBG20N18 HTGB LIFE
11
IGSSR tested at -4V

## Slide 12
FBG20N18 HTGB LIFE
12
RDSON at 18A VGS@5V

## Slide 13
FBG20N18 HTGB LIFE
13
Vgsth at 3mA