## Slide 1: FBG10N30BSH Reliability Data
5/1/24

## Slide 2
FBG10N30BSH Circuit
The circuit was not optimized for efficiency but rather to demonstrate the stability of device and Rdson.
FBG20N18
Or
FBG10N30
Simplified High Side Buck converter circuit
FBG20N18
GAM01 Driver

## Slide 3
Tested variations of VDS voltage, IDS current and Switching Frequency in a high side buck converter over a 2000+ hours time and across 3 wafer lots.
  VDS tested : 60V and 90V ( 10% over 80% VDS requirement) measured at Power supply and does not include any overshoot occurring at the DUT due to the buck circuit performance.
  Iout tested : 1A, 4.5A
  Parts tested with full parametric test at interim steps 48,hrs, 120hrs, 260hrs, 500hrs, 1000hrs, 2000hrs, 3000hrs.
  No failures have been observed.
FBG10N30BSH Switching Life Test

## Slide 4
EFFICIENCY at 500kHz VDS=60V -90V Io=1A

## Slide 5
EFFICIENCY at 100kHz VDS=60V -90V Io=1A

## Slide 6
EFFICIENCY at 100kHz VDS=60V -90V Io=4.5A

## Slide 7
Lab window left open over the weekend, and it was snowing in Massachusetts.
EFFICIENCY at 500kHz VDS=60V Io=7.5A

## Slide 8
Tested variations of VDS and VGS voltages over several temperatures over a 2000Hrs timeframe
  VDS Tested : 110V, 120V, 130V at Temperatures of 120C
  VGS Tested : 5V, 6V, 6.75V at Temperatures of 110C and 150C
  Parts tested with full parametric test at interim steps 24hrs, 48,hrs, 96hrs, 210hrs, 500hrs, 1000hrs, 1500hrs, 2000hrs
  Parts with very high leakage were removed at each step
  X axis (voltage represents Applied stress voltage not test voltage)
FBG10N30BSH DC LIFE TEST

## Slide 9
FBG10N30 HTGB LIFE
9

## Slide 10
FBG10N30 HTGB LIFE
10

## Slide 11
FBG10N30 HTGB LIFE
11

## Slide 12
FBG10N30 HTGB LIFE
12

## Slide 13
FBG10N30 HTRB LIFE
13

## Slide 14
14
FBG10N30 HTRB LIFE

## Slide 15
15
FBG10N30 HTRB LIFE

## Slide 16
16
FBG10N30 HTRB LIFE

## Slide 17
17
FBG10N30 HTRB LIFE