## Slide 1: VDS STRESS TEST

## Slide 2
Physics of Failure Testing FBG20N18
Test purpose: To expose devices to a range of DC and AC (Operating) stressors to evaluate capability and inform lifetime modeling of the 200V product platform
Life Switching Testing : Tested variations of VDS voltage, IDS current and Switching Frequency in a high side buck converter over a 2000Hrs time
VDS tested : 140V and 170V (Nominal) measured at Power supply and does not include any overshoot occurring at the DUT due to the buck circuit performance.
Iout tested : 1A, 3A
Stress Switching Testing : Tested variations of VDS voltage, IDS current and Switching Frequency in a high side buck converter over multiple 20Hour test times
VDS Tested : 60 to 240V (Nominal) measured at Power supply and does not include any overshoot occurring at the DUT due to the buck circuit performance.
Iout tested : 1 to 9A current limited by heat dissipation
Life DC Testing : Tested variations of VDS and VGS voltages over several temperatures over a 2000Hrs timeframe
VDS Tested : 200V, 230V, 250V at Temperatures of 100C and 130C
VGS Tested : 6V, 6.75V, 7.25V at Temperatures of 100C and 150C
Stress DC Testing: Tested variations of VDS and VGS voltages over temperature over multiple 20 hour test times
VDS tested : 160V to 300V at Temperatures of 110C, 130C, 150C
VGS Tested : 4V to 8.25V at Temperatures of 110C, 130C, and 150C

## Slide 3: Switching LIFE
Parts were run for 2000hrs at selected conditions
  Parts tested with full parametric test on Focused tester at interim steps 48,hrs, 120hrs, 260hrs, 500hrs, 1000hrs, 2000hrs
  No failures have been observed so far thru 1500hrs

## Slide 4: POF Life/Stress Switching Test Boards
Mux outputs.
Measure Iin, Iout, and Vout
Also measure DUT Temp
Clock distribution adds delay along the devices
Odd devices are 0deg and even are 180deg
Sig Gen in
0 deg and 180deg
Device loads are external
Main Bus Power In

## Slide 5: 200V POF SWITCHING LIFE TEST RACK
140V
170V
Rack 5- 500Khz 1A
Rack 6- 100Khz 1A
Rack 7- 100Khz 4A
Rack 8- 500Khz 3A

## Slide 6: DUT Simplified Schematic

## Slide 7: 20N18 Efficiency Normalized
Take away : Efficiency dependent to drain voltage no current dependence .
Temperature seems to slow down the Drdson effect thru annealing . ( more pronounced on 100V device analysis)

## Slide 8: 20N18 Efficiency (raw data)

## Slide 9: RDSON NORMALIZED
Take away : Rdson dependent to drain voltage no current dependence correlate to efficiency
Temperature seems to slow down the Drdson effect thru annealing . ( more pronounced on 100V device analysis)

## Slide 10: RDSON
Take away : Efficiency dependent to drain voltage no current dependence .
Temperature seems to slow down the Drdson effect thru annealing . ( more pronounced on 100V device analysis)

## Slide 11: DRON Normalized
Take away : Drdon does not correlate to efficiency.
fast traps do nt seem to increase with longer stress compared to the slow traps (Rdson)

## Slide 12: DRON

## Slide 13: Vth Normalized
VTh performed pre Drdson and Idss on the Focused tester.
Initial shift but stable

## Slide 14: Vth (raw data)

## Slide 15: Vth-Post RDSON Test
VTh performed after Drdson and Idss on the Focused tester. Data
Talk to Rob S.

## Slide 16: Vth-POST-PRE DELTA

## Slide 17: IDSS
Leakages not affected

## Slide 18: IGSS
Leakages not affected

## Slide 19: Switching STRESS
Parts were grouped and run at successively higher voltage.
  Test period was ~18 hours (Overnight)
  Parts tested with full parametric test on Focused tester after every step.
  Parts with very high leakage were removed at each step
  X axis (voltage represents Applied stress voltage not test voltage)

## Slide 20: Case temps and SOA limits
Take away : Switching losses are driving Case temp more than current

## Slide 21: Switching Stress Parametric

## Slide 22: Switching Stress Parametric

## Slide 23: DC STRESS
Parts were grouped and run at successively higher voltage.
  Test period was ~18 hours (Overnight)
  Parts tested with full parametric test on Focused tester after every step.
  Parts with very high leakage were removed at each step
  X axis (voltage represents Applied stress voltage not test voltage)

## Slide 24
HTRB OVEN LOGS

## Slide 25
HTGB OVEN LOGS

## Slide 26
IDSS - HTGB
VDS test voltage is 200V for all data points

## Slide 27
IGSSF - HTGB
VGS test voltage is 5V for all data points

## Slide 28
IGSSR - HTGB
VGS test voltage is -4V for all data points

## Slide 29
VGSth - HTGB
Vgs th test is @ 3mA all data points

## Slide 30
RDSON - HTGB
This drop caused by FTI fixture change
RDSON test is @ 18A, Vgs=5V
all data points

## Slide 31
RDSON 1s - HTGB
This drop caused by FTI fixture change
RDSON test is @ 18A, Vgs=5V
all data points

## Slide 32
DYNAMIC RON PRE STRESS - HTGB
This drop caused by FTI fixture change
DRON test is @ 15A, Vgs=5V
all data points.
10sec stress at 160V, test follows at
6-8us after stress

## Slide 33
DYNAMIC RON POST STRESS - HTGB
DRON test is @ 15A, Vgs=5V
all data points.
DRON test is @ 15A, Vgs=5V
all data points.
10sec stress at 160V, test follows at
6-8us after stress

## Slide 34
DYNAMIC RON % - HTGB
DRON test is @ 15A, Vgs=5V
all data points.
10sec stress at 160V, test follows at
6-8us after stress. Pre test @15A

## Slide 35
IDSS - HTRB
VDS test voltage is 200V for all data points

## Slide 36
IGSSF - HTRB
VGS test voltage is 5V for all data points

## Slide 37
IGSSR - HTRB
VGS test voltage is -4V for all data points

## Slide 38
VGSth - HTRB
Vgs th test is @ 3mA all data points

## Slide 39
RDSON - HTRB
This drop caused by FTI fixture change.
Drop at 300V caused by annealing due to fuse
failure / low bias during oven exposure
RDSON test is @ 18A, Vgs=5V
all data points

## Slide 40
RDSON 1s - HTRB
This drop caused by FTI fixture change.
Drop at 300V caused by annealing due to fuse
failure / low bias during oven exposure
RDSON test is @ 18A, Vgs=5V
all data points

## Slide 41
DYNAMIC RON PRE STRESS - HTRB
This drop caused by FTI fixture change.
Drop at 300V caused by annealing due to fuse
failure / low bias during oven exposure
DRON test is @ 15A, Vgs=5V
all data points.
10sec stress at 160V, test follows at
6-8us after stress

## Slide 42
DYNAMIC RON POST STRESS - HTRB
This drop caused by FTI fixture change.
Drop at 300V caused by annealing due to fuse
failure / low bias during oven exposure
DRON test is @ 15A, Vgs=5V
all data points.
10sec stress at 160V, test follows at
6-8us after stress

## Slide 43
DYNAMIC RON % - HTRB
DRON test is @ 15A, Vgs=5V
all data points.
10sec stress at 160V, test follows at
6-8us after stress

## Slide 44
OVEN LOG SUMMARY
 | HTRB Voltage | Current (mA) | # Parts | Avg Power per part | Notes | HTGB Voltage | Current (mA) | # Parts | Avg Power per part | Notes
110C | 160 | 0.141 | 10 | 0.002 |  | 4 | 0.023 | 10 | 0.0000 | 
 | 180 | 0.198 | 10 | 0.004 |  | 5 | 0.056 | 10 | 0.0000 | 
 | 200 | 0.212 | 10 | 0.004 |  | 6 | 0.144 | 10 | 0.0001 | 
 | 210 | 0.125 | 10 | 0.003 |  | 6.25 | 0.28 | 10 | 0.0002 | 
 | 220 | 0.11 | 10 | 0.002 |  | 6.5 | 0.4 | 10 | 0.0003 | 
 | 230 | 0.131 | 10 | 0.003 | 1 part failed | 6.75 | 0.7 | 10 | 0.0005 | 
 | 240 | 0.134 | 9 | 0.004 |  | 7 | 1.45 | 10 | 0.0010 | 
 | 250 | 0.155 | 9 | 0.004 |  | 7.25 | 2.1 | 10 | 0.0015 | 
 | 260 | 0.145 | 9 | 0.004 |  | 7.5 | 3.1 | 10 | 0.0023 | 
 | 270 | 0.1 | 9 | 0.003 | 1 part failed blew DMM fuse | 7.75 | 4.5 | 10 | 0.0035 | 
 | 280 | 0.1 | 8 | 0.004 |  | 8 | 7 | 10 | 0.0056 | 2 parts failed
 | 290 | 0.1 | 8 | 0.004 |  | 8.25 | 7 | 8 | 0.0072 | 2 parts failed
 | 300 | 0.1 | 8 | 0.004 | 1 part failed shorted supply | 8.5 | 27 | 6 | 0.0383 | 3 parts failed+ 1 part fails IGSS
130C | 160 | 0.3 | 10 | 0.005 |  | 4 | 0.05 | 10 | 0.0000 | 
 | 180 | 0.3 | 10 | 0.005 |  | 5 | 0.1 | 10 | 0.0001 | 
 | 200 | 0.31 | 10 | 0.006 | 1 part failed/replaced - Fixture possible | 6 | 0.4 | 10 | 0.0002 | 
 | 210 | 0.29 | 10 | 0.006 | 1 part failed Fixture Possible | 6.25 | 0.63 | 10 | 0.0004 | 
 | 220 | 0.28 | 9 | 0.007 |  | 6.5 | 1.15 | 10 | 0.0007 | 
 | 230 | 0.28 | 9 | 0.007 | 1 part failed Fixture Possible | 6.75 | 1.53 | 10 | 0.0010 | 
 | 240 | 0.33 | 8 | 0.010 |  | 7 | 2.5 | 10 | 0.0018 | 
 | 250 | 0.35 | 8 | 0.011 |  | 7.25 | 3.8 | 10 | 0.0028 | 
 | 260 | 0.51 | 8 | 0.017 | 1 part failed | 7.5 | 6.4 | 10 | 0.0048 | 
 | 270 | 0.32 | 7 | 0.012 | 1 part failed | 7.75 | 8.3 | 10 | 0.0064 | 1 part failed
 |  |  |  |  |  | 8 | 8.6 | 9 | 0.0076 | 2 parts failed
 |  |  |  |  |  | 8.25 | 8.4 | 7 | 0.0099 | 3 parts failed
 |  |  |  |  |  | 8.5 | 5.1 | 4 | 0.011 | 1 part failed + 2 fail IGSS

## Slide 45
OVEN LOG SUMMARY
 | HTRB Voltage | Current (mA) | # Parts | Avg Power per part | Notes | HTGB Voltage | Current (mA) | # Parts | Avg Power per part | Notes
150C | 160 | 0.692 | 10 | 0.011 | ` | 4 | 0.1 | 10 | 0.000 | 
 | 180 | 0.719 | 10 | 0.013 |  | 5 | 0.16 | 10 | 0.000 | 
 | 200 | 0.747 | 10 | 0.015 |  | 6 | 0.45 | 10 | 0.000 | 
 | 210 | 0.76 | 10 | 0.016 | 2 parts failed | 6.25 | 0.71 | 10 | 0.000 | 
 | 220 | 0.621 | 8 | 0.017 |  | 6.5 | 1.07 | 10 | 0.001 | 
 | 230 | 0.647 | 8 | 0.019 | 1 part failed | 6.75 | 1.64 | 10 | 0.001 | 
 | 240 | 0.617 | 7 | 0.021 |  | 7 | 2.45 | 10 | 0.002 | 
 | 250 | 0.631 | 7 | 0.023 |  | 7.25 | 3.68 | 10 | 0.003 | 
 | 260 | 0.653 | 7 | 0.024 | 1 part failed | 7.5 | 9.26 | 10 | 0.007 | 1 part fails IGSS
 | 270 | 0.593 | 6 | 0.027 |  | 7.75 | 11.6 | 10 | 0.009 | 1 part failed
 | 280 | 0.616 | 6 | 0.029 | 1 part failed | 8 | 47.7 | 9 | 0.042 | 3 parts fail IGSS
 |  |  |  |  |  | 8.25 | 114 | 9 | 0.105 | 1 part fails IGSS

## Slide 46
HTRB FAILURE XRAY
110C-#5 – 230V
110C-#9 – 270V

## Slide 47
HTRB FAILURE XRAY
130C-#17 – 200V
130C-#22 – 210V
130C-#15 – 230V
130C-#13 – 260V

## Slide 48
HTRB FAILURE XRAY
150C-#28 – 210V
150C-#36 – 280V
150C-#30 – 210V
150C-#33 – 260V
150C-#37 – 230V

## Slide 49
STRESS FAILURE SUMMARY
20N18 - STRESS Sumary |  |  |  |  | 
Temp | SN | Stress V | Notes | Action | Notes / Final Screening Value
110C | 7,8 | 8 | High Gate Leakage |  | 
 | 10 | 8.25 | High Gate Leakage |  | 
 | 11 | 8.25 | High Gate Leakage low Vgsth |  | 
 | 2,3,4,5 | 8.5 | High Gate Leakage |  | 
 | 5 | 230 | Vgsth Low high G and D Leakage |  | Possibel Fixture related
 | 9 | 270 | Vgsth Low high G and D Leakage |  | 
 | 14 | 300 | Vgsth Low high G and D Leakage |  | 
130C | 19 | 7.75 | High Leakage low Vgsth |  | 
 | 16, 19 | 8 | High Vgsth High gate leakage |  | 
 | 21,20 | 8.25 | Vgsth Low high G and D Leakage |  | 
 | 18 | 8.5 | High Vgsth High gate leakage |  | 
 | 17 | 200 | Low Vgs th High G and D Leakage |  | Possibel Fixture related
 | 22 | 210 | Low Vgs th High G and D Leakage |  | Possibel Fixture related
 | 15 | 230 | Low Vgs th High G and D Leakage |  | Possibel Fixture related
 | 13 | 260 | Low Vgs th High G and D Leakage |  | 
 | 27 | 270 | Low Vgs th High G and D Leakage |  | 
150C | 37 | 7.5 | High IGSS |  | 
 | 25 | 7.75 | Vgsth Low high G and D Leakage |  | 
 | 35,27,28 | 8 | High Gate Leakage |  | 
 | 37, 29 | 8.25 | High Gate Leakage |  | 
 | 28,30 | 210 | Vgsth Low high G and D Leakage |  | 
 | 37 | 230 | Vgsth Low high G and D Leakage |  | 
 | 33 | 260 | Vgsth Low high G and D Leakage |  | 
 | 36 | 280 | Vgsth Low high G and D Leakage |  | 

## Slide 50: DC LIFE
Parts were run for 2000hrs at selected conditions
  Parts tested with full parametric test on Focused tester at interim steps 24hrs, 48,hrs, 96hrs, 210hrs, 500hrs, 1000hrs, 1500hrs, 2000hrs
  Parts with very high leakage were removed at each step
  X axis (voltage represents Applied stress voltage not test voltage)

## Slide 51: OVEN LOGS

## Slide 52: HTGB LIFE
IDSS tested at 200V

## Slide 53: HTGB LIFE
IGSSF tested at 5V

## Slide 54: HTGB
IGSSR tested at -4V

## Slide 55: HTGB
DRON pre at 15A VGS@5V

## Slide 56: HTGB
DRON post at 15A VGS@5V
10s stress at 160V followed by
Test at 5-8us after removal

## Slide 57: HTGB
RDSON at 18A VGS@5V

## Slide 58: HTGB
Vgsth at 3mA

## Slide 59: HTRB
IDSS tested at 200V

## Slide 60: HTRB
IGSS tested at 5V

## Slide 61: HTRB
IGSR tested at -4V

## Slide 62: HTRB
DRON pre at 15A VGS@5V

## Slide 63: HTRB
DRON post at 15A VGS@5V
10s stress at 160V followed by
Test at 5-8us after removal

## Slide 64: HTRB
RDSON at 18A VGS@5V

## Slide 65: HTRB
Vgsth at 3mA

## Slide 66: LIFE TEST SUMMARY HTGB
Temp | Stress V | Time(Hrs) | SN | Wafer # | Notes
100C | 6.75 |  |  |  | 
 |  | 1479 | 68 | Q211 | High IGSS, still functional-part was OOF
 |  | 2020 | 126 | Y003 | High IGSS, still functional-OOF replacemnt actual hours 1924
 | 7.25 | 96 | 81 | Q211 | Out of Family, High IGSS,IDSS, Vth - Part was OOF
 |  | 500 | 16 | Y046 | High IGSS -removed 1000Hrs
 |  | 1000 | 55 | Y003 | High IGSS, still functional
 |  |  | 60 | Q211 | High IGSS -removed 1000Hrs
 |  |  | 127 | Y003 | High IGSS, still functional
 |  | 1479 | 70 | Q211 | High IGSS, still functional-OOF replacment actual hours 1383
 |  | 2020 | 53 | Y003 | High IGSS, Vth, Idss nonfunctional
 |  |  | 59 | Q211 | High IGSS, Vth, Idss nonfunctional=Part was OOF
 |  |  | 61 | Q211 | High IGSS, low Vth, high Idss nonfunctional
 |  |  | 17 | Y046 | High IGSS, low Vth, high Idss nonfunctional
 |  | 2188 | 13 | Y046 | High IGSS, still functional
Temp | Stress V | Time(Hrs) | SN | Wafer # | Notes
150C | 6V |  |  |  | 
 | 6.75 | 1000 | 85 | Y003 | High IGSS, still functional
 |  | 2020 | 33 | Y046 | High IGSS, high Vth still functional
 |  | 2188 | 29 | Y046 | High Gate and Drain, Fuse Blew Pulled.
 | 7.25 | 48 | 39 | Q211 | High IGSS, still functional
 |  |  | 40 | Y046 | High IGSS, still functional
 |  | 138 | 37 | Y046 | High IGSS, IDSS, Low Vth
 |  | 210 | 42 | Q211 | High IGSS, still functional
 |  |  | 34 | Y046 | High IGSS, still functional-removed 100Hrs
 |  | 500 | 78 | Y003 | High IGSS, IDSS, High Vth
 |  | 1000 | 43 | Q211 | High IGSS, still functional
 |  |  | 44 | Q211 | High IGSS, still functional
 |  |  | 84 | Q211 | High IGSS, still functional
 |  |  | 35 | Y046 | High IGSS, still functional-removed 100Hrs
 |  |  | 40 | Y046 | High IGSS, still functional-removed 100Hrs
 |  |  | 75 | Y003 | High IGSS, still functional
 |  |  | 79 | Y003 | High IGSS, still functional-removed 100Hrs
 |  | 1479 | 130 | Y003 | High IGSS, still functional
 |  |  | 36 | Y046 | High IGSS, still functional
 |  | 2020 |  |  | No New Failures - 4 surviving parts 1 of which was OOF

## Slide 67: LIFE TEST SUMMARY HTRB
Temp | Stress V | Time(Hrs) | SN | Wafer # | Notes
100C | 200V |  |  |  | 
 | 230V | 1020 | 94 | Y003 | Fuse blown, pulled
 |  | 1526 | 90 | Y003 | Fuse blown, pulled
 |  |  | 110 | Q211 | Fuse blown, pulled
 | 250V | 24 | 119 | Q211 | Fuse blown, pulled
 |  | 48 | 121 | Y003 | Fuse blown, pulled
 |  | 500 | 117 | Q211 | Fuse blown, pulled
 |  | 1020 | 100 | Y003 | Fuse blown, pulled
 |  | 1526 | 101 | Y003 | Fuse blown, pulled
 |  | 2048 | 121 | Q211 | Fuse blown, pulled
 |  |  | 123 | Q211 | Fuse blown, pulled
Temp | Stress V | Time(Hrs) | SN | Wafer # | Notes
130C | 200V | 24 | 120 | Y003 | Fuse blown, pulled
 |  | 500 | 102 | Y003 | Fuse blown, pulled
 |  | 1020 | 105 | Y003 | Fuse blown, pulled
 |  | 1426 | 107 | Y003 | Fuse blown, pulled
 |  |  | 130 | Q211 | Fuse blown, pulled
 | 230V | 48 | 140 | Q211 | Fuse blown, pulled
 |  | 210 | 109 | Y003 | Fuse blown, pulled
 |  | 500 | 112 | Y003 | Fuse blown, pulled
 |  | 1020 | 119 | Y003 | Fuse blown, pulled
 |  | 1526 | 74 | Q211 | Fuse blown, pulled
 |  |  | 138 | Q211 | Fuse blown, pulled
* | No failures seen from wafer Y046 |  |  |  | 

## Slide 68: HTRB Failures XRAY 230V 100C
Y003 #94-PRE-POST
Q211 #110-PRE-POST
Y003 #90-PRE-POST

## Slide 69: HTRB Failures XRAY 250V 100C
Y003 #121-PRE POST
Q211 #119-PRE POST
Q211 #117-PRE POST

## Slide 70
HTRB Failures XRAY 250V 100C
Q211 #121-PRE POST
Y003 #100-PRE POST
Y003 #101-PRE POST

## Slide 71
HTRB Failures XRAY 250V 100C
Q211 #123-PRE POST

## Slide 72: HTRB Failures XRAY 200V 130C
Y003 #120-PRE POST
Y003 #102-PRE POST
Y003 #105-PRE POST

## Slide 73: HTRB Failures XRAY 200V 130C
Y003 #107-PRE POST
Q211 #130-PRE POST

## Slide 74: HTRB Failures XRAY 230V 130C
Q211 #140-PRE POST
Y003 #109-PRE POST
Y003 #112-PRE POST

## Slide 75: HTRB Failures XRAY 230V 130C
Y003 #119-PRE POST
Q211 #138-PRE POST
Q211 #74-PRE POST