## Slide 1: VGS STRESS TEST FBG10N30

## Slide 2: DC STRESS
Parts were grouped and run at successively higher voltage.
Stress DC Testing: Tested variations of VGS voltages over temperature over multiple 20 hours test times
VGS Tested : 4V to 8V at Temperatures of 110C, 130C, 150C, 170C
Test period was ~18 hours (Overnight)
Parts tested with full parametric test on Focused tester after every step.
Parts with very high leakage were removed at each step
X axis (voltage represents Applied stress voltage not test voltage)

## Slide 3
HTRB OVEN LOGS

## Slide 4
HTGB OVEN LOGS

## Slide 5
IDSS - HTGB Stress Voltage
VDS test voltage is 100V for all data points

## Slide 6
IGSSF - HTGB Stress Voltage
VGS test voltage is 5V for all data points

## Slide 7
IGSSR - HTGB Stress Voltage
VGS test voltage is
-4V for all data points

## Slide 8
VGSth - HTGB Stress Voltage
Vgs th measured at 5mA

## Slide 9
RDSON - HTGB Stress Voltage
RDSON measured at 30A, Vgs 5V

## Slide 10
RDSON 1s - HTGB Stress Voltage
RDSON measured at 30A, Vgs 5V

## Slide 11
DYNAMIC RON PRE STRESS - HTGB Stress Voltage
RON measured at 15A, Vgs 5V

## Slide 12
DYNAMIC RON POST STRESS - HTGB Stress Voltage
RON measured at 15A, Vgs 5V

## Slide 13
DYNAMIC RON % - HTGB Stress Voltage