## Slide 1: SWITCHING Life TEST FBG10N30

## Slide 2: Switching LIFE
Tested variations of VDS voltage, IDS current and Switching Frequency in a high side buck converter over a 2000Hrs time
  VDS tested : 40V, 60V and 90V (Nominal) measured at Power supply and does not include any overshoot occurring at the DUT due to the buck circuit performance.
  Iout tested : 1A, 4A, 7.5A
  Parts tested with full parametric test at interim steps 48,hrs, 120hrs, 260hrs, 500hrs, 1000hrs, 2000hrs
  No failures have been observed

## Slide 3: 10N30 Efficiency Normalized
Take away : Efficiency dependent to drain voltage no current dependence .
Temperature seems to slow down the Drdson effect thru annealing .

## Slide 4: 10N30 Efficiency (raw data)

## Slide 5: RDSON Normalized

## Slide 6: RDSON

## Slide 7: DRON Normalized

## Slide 8: DRON

## Slide 9: Vth NORMALIZED

## Slide 10: Vth (raw data)

## Slide 11: Vth-POST RDSON Test

## Slide 12: Vth-POST-PRE DELTA

## Slide 13: IDSS

## Slide 14: IGSS