## Slide 1: SWITCHING Life TEST FBG20N18

## Slide 2: Switching LIFE
Tested variations of VDS voltage, IDS current and Switching Frequency in a high side buck converter over a 2000Hrs time
  VDS tested : 140V and 170V (Nominal) measured at Power supply and does not include any overshoot occurring at the DUT due to the buck circuit performance.
  Iout tested : 1A, 3A
  Parts tested with full parametric test on Focused tester at interim steps 48,hrs, 120hrs, 260hrs, 500hrs, 1000hrs, 2000hrs
  No failures have been observed so far thru 1500hrs

## Slide 3: 20N18 Efficiency Normalized
Take away : Efficiency dependent to drain voltage no current dependence .
Temperature seems to slow down the Drdson effect thru annealing . ( more pronounced on 100V device analysis)

## Slide 4: 20N18 Efficiency (raw data)

## Slide 5: RDSON NORMALIZED
Take away : Rdson dependent to drain voltage no current dependence correlate to efficiency
Temperature seems to slow down the Drdson effect thru annealing . ( more pronounced on 100V device analysis)

## Slide 6: RDSON
Take away : Efficiency dependent to drain voltage no current dependence .
Temperature seems to slow down the Drdson effect thru annealing . ( more pronounced on 100V device analysis)

## Slide 7: DRON Normalized
Take away : Drdon does not correlate to efficiency.
fast traps do nt seem to increase with longer stress compared to the slow traps (Rdson)

## Slide 8: DRON

## Slide 9: Vth Normalized
VTh performed pre Drdson and Idss on the Focused tester.
Initial shift but stable

## Slide 10: Vth (raw data)

## Slide 11: Vth-Post RDSON Test
VTh performed after Drdson and Idss on the Focused tester. Data
Talk to Rob S.

## Slide 12: Vth-POST-PRE DELTA

## Slide 13: IDSS
Leakages not affected

## Slide 14: IGSS
Leakages not affected